**TECHNICAL DATA SHEET**

|  |  |  |  |
| --- | --- | --- | --- |
| **PRODUCT DESCRIPTION** | | | |
| **PRODUCT NAME: EURO GULF0 MOTOR OIL SAE 25W60** | | | |
| **SPECIFICATIONS** | | | |
| **API: SN** | | | |
|  | **TESTS** | **METHOD** | **TYPICAL RESULTS** |
| APPEARANCE | VISUAL | Bright & Clear |
| DENSITY @ 15°C, g/cm3 | ASTM D1298 | 0.8834 |
| KINEMATIC VISCOSITY @ 40°C, cSt | ASTM D445 | 229.82 |
| KINEMATIC VISCOSITY @ 100°C, cSt | ASTMD445 | 23.17 |
| VISCOSITY INDEX | ASTM D2270 | 125 |
| FLASH POINT, °C | ASTM D92 | Min. 220 |
| POUR POINT, °C | ASTM D97 | -18 |
| TBN, mgKOH/g | ASTM D2896 | 7.3 |
| Tests has been conducted in accordance with internationally accepted methods such as ASTM standards | | |